CEDCP: The Collection of Experimental Data on Composite Properties.

# Electrical conductivity data
Data has been converted to S/m
	Reference	Matrix material	Filler material	Aspect ratio	File name
1	Agari (1991) [1]	Polyethylene, 2.5·10-14 S/cm	Carbon fiber, 3.3-6.3·102 S/cm	1.0	Agari1991Fig4Curv1.inp
2	Agari (1991) [1]	Polyethylene, 2.5·10-14 S/cm	Carbon fiber, 3.3-6.3·102 S/cm	6.0	Agari1991Fig4Curv2.inp
3	Agari (1991) [1]	Polyethylene, 2.5·10-14 S/cm	Carbon fiber, 3.3-6.3·102 S/cm	21.6	Agari1991Fig4Curv3.inp
4	Agari (1991) [1]	Polyethylene, 2.5·10-14 S/cm	Carbon fiber, 3.3-6.3·102 S/cm	45.3	Agari1991Fig4Curv4.inp
5	Aribou (2019) [2]	Diglycidylic Ether of Bisphenol F, 1.4·10-16 S/cm	Carbon black Raven 2000, 6.56 S/cm	1.0	Aribou2019Fig3a.inp
6	Aribou (2019) [2]	Diglycidylic Ether of Bisphenol F, 1.4·10-16 S/cm	Carbon black Raven 7000, 3.50 S/cm	1.0	Aribou2019Fig3b.inp
7	Landauer (1952) [3]	Bismuth, 7.7·105 S/m	Tin, 9.1·106 S/m	1.0	Landauer1952Fig5.inp
8	Wu (1997) [4]	Boron nitride, 1.0-14 S/m, 2.381-13 S/m	Graphite powder, 833.333 S/m, 34722.222 S/m	1.0	WuMcLachlan1997Fig1a.inp
9	Wu (1997) [4]	Boron nitride, 1.0-14 S/m, 2.381-13 S/m	Graphite powder, 833.333 S/m, 34722.222 S/m	1.0	WuMcLachlan1997Fig1b.inp
10	Wu (1997) [4]	Boron nitride, 1.0-14 S/m, 2.381-13 S/m	Graphite powder, 833.333 S/m, 34722.222 S/m	1.0	WuMcLachlan1997Fig3.inp
11	Sanchez (2018) [5]	Chitosan	Hydroxyapatite nanoparticles	1.0	Sanchez2018Fig7a.inp
12	Janget (2015) [6]	Polydimethylsiloxane (PDMS), 2.5e-14 S/m	multi-walled CNT, 100 S/m?	1250	Jang2015Fig8Cond.inp
13	Wang (2012) [7]	PVDF	Fe3O4	1.0	Wang2012Fig4Cond100Hz.inp
14	Chiarello (2005) [8]	Portland cement / (type I, 52.5 R),	Carbon fiber	750.0	Chiarello2005Fig6mm6.inp
15	Chiarello (2005) [8]	Portland cement / (type I, 52.5 R),	Carbon fiber	375.0	Chiarello2005Fig6mm3.inp
16	Chiarello (2005) [8]	Portland cement / (type I, 52.5 R),	Carbon fiber	0.5	Chiarello2005Fig6um4.inp
17	Mamunya (2002) [9]	PVC, 1e-13.5 S/m	Cu, 1e+5.8 S/m	1.0	mamunya2002Fig6Curv1.inp
18	Mamunya (2002) [9]	Epoxy resin, 1e-12.8 S/m	Cu, 1e+5.2 S/m	1.0	mamunya2002Fig6Curv2.inp
19	Mamunya (2002) [9]	PVC, 1e-13.5 S/m	Ni, 1e+4.5 S/m	1.0	mamunya2002Fig6Curv3.inp
20	Mamunya (2002) [9]	Epoxy resin, 1e-12.8 S/m	Ni, 1e+4.8 S/m	1.0	mamunya2002Fig6Curv4.inp
21	Kim (2005) [10]	Epoxy resin	Multiwalled carbon nanotubes	2000.0	Kim2005Fig5a.inp
22	Kim (2005) [10]	Epoxy resin	Multiwalled carbon nanotubes	2000.0	Kim2005Fig5b.inp
23	Barrau (2003) [11]	Epoxy resin, 7.9×10-16 S/cm	Carbon nanotubes	7500.0	Barrau2003Fig2a.inp
24	Barrau (2003) [11]	Epoxy resin, 7.9×10-16 S/cm	Carbon nanotubes	7500.0	Barrau2003Fig2b.inp
25	Clingerman (2002) [12]	Nylon 6,6 (Zytel 101 NC010), 10-15 S/cm	3.175-mm chopped PAN carbon fiber	13.678	Clingerman2002Fig1AN.inp
26	Clingerman (2002) [12]	Polycarbonate (Lexan HF1110-111N) 10-17 S/cm	3.175-mm chopped PAN carbon fiber	19.442	Clingerman2002Fig1AP.inp
27	Clingerman (2002) [12]	Nylon 6,6 (Zytel 101 NC010), 10-15 S/cm	200-mm milled PAN carbon fiber	9.546	Clingerman2002Fig1BN.inp
28	Clingerman (2002) [12]	Polycarbonate (Lexan HF1110-111N) 10-17 S/cm	200-mm milled PAN carbon fiber	10.751	Clingerman2002Fig1BP.inp
29	Clingerman (2002) [12]	Nylon 6,6 (Zytel 101 NC010), 10-15 S/cm	ThermocarbTM Specialty Graphite	1.0	Clingerman2002Fig1FN.inp
30	Clingerman (2002) [12]	Polycarbonate (Lexan HF1110-111N) 10-17 S/cm	ThermocarbTM Specialty Graphite	1.0	Clingerman2002Fig1FP.inp
31	Clingerman (2002) [12]	Nylon 6,6 (Zytel 101 NC010), 10-15 S/cm	Ni-coated PAN carbon fiber	23.821	Clingerman2002Fig1GN.inp
32	Clingerman (2002) [12]	Polycarbonate (Lexan HF1110-111N) 10-17 S/cm	Ni-coated PAN carbon fiber	17.412	Clingerman2002Fig1GP.inp
33	Mamunya (1996) [13]	Polypropylene	Carbon black	1.0	mamunya1996Fig2PP.inp
34	Mamunya (1996) [13]	Polyethylene	Carbon black	1.0	mamunya1996Fig2PE.inp
35	Mamunya (1996) [13]	Polystyrene	Carbon black	1.0	mamunya1996Fig2PS.inp
36	Mamunya (1996) [13]	Poly(methyl)methacrylate	Carbon black	1.0	mamunya1996Fig2PMMA.inp
37	Mamunya (1996) [13]	Polyamide	Carbon black	1.0	mamunya1996Fig2PA.inp
38	Mamunya (1996) [13]	Polypropylene	carbon black	1.0	mamunya1996Fig3PP1.inp
39	Mamunya (1996) [13]	Polyethylene	carbon black	1.0	mamunya1996Fig3PE1.inp
40	Gojny (2006) [14]	DGEBA-based epoxy resin	Carbon black	1.0	Gojny2006Fig3CB.inp
41	Gojny (2006) [14]	DGEBA-based epoxy resin	SWCNT Elicarb	5000.0	Gojny2006Fig3SWCNT.inp
42	Gojny (2006) [14]	DGEBA-based epoxy resin	DWCNT	3571.4	Gojny2006Fig3DWCNT.inp
43	Gojny (2006) [14]	DGEBA-based epoxy resin	DWCNT-NH2 (~1%)	1428.6	Gojny2006Fig3DWCNT-NH2.inp
44	Gojny (2006) [14]	DGEBA-based epoxy resin	MWCNT	3333.3	Gojny2006Fig3MWCNT.inp
45	Gojny (2006) [14]	DGEBA-based epoxy resin	MWCNT-NH2 (~1%)	266.7	Gojny2006Fig3MWCNT-NH2.inp
46	Maiti (2013) [15]	Polycarbonate and acrylonitrile butadiene styrene	MWCNT	157.9	Maiti2013Fig2a.inp
47	Yousefi (2012) [16]	Polyurethane	Reduced graphene oxide	10000.0	Yousefi2012Fig9.inp
48	Stankovich (2006) [17]	Polystyrene	Graphene sheets	1000.0	Stankovich2006Fig3.inp
49	Zhang (2010) [18]	Polyethylene terephthalate	Graphene nanosheets	146.0	Zhang2010Fig5gn.inp
50	Zhang (2010) [18]	Polyethylene terephthalate	Graphite flake	36.0	Zhang2010Fig5gt.inp
51	Prokhorov (2023) [20]	Chitosan	Graphene oxide sheets, water 24%	150.0	Prokhorov2023Fig5aW24.inp
52	Prokhorov (2023) [20]	Chitosan	Graphene oxide sheets, water 9%	150.0	Prokhorov2023Fig5aW24.inp
53	Prokhorov (2019) [22]	Chitosan	Copper nanocomposites	1.0	Prokhorov2023Fig6a.inp
54	Sanches (2019) [23]	Chitosan	non-functionalized MWCNT	666.7	Sanches2019Fig7nf.inp
55	Sanches (2019) [23]	Chitosan	MWCNTs functionalized by chemical oxidation in HNO3	666.7	Sanches2019Fig7HNO3.inp
56	Sanches (2019) [23]	Chitosan	carboxyl-terminated MWCNTs	666.7	Sanches2019Fig7carb.inp
57	Li (2008) [26]	Polyvinylidene fluoride (PVDF)	Multi-walled carbon nanotubes (MWCN)	2000.0	Li2008Fig5a.inp
58	Li (2008) [26]	Polyvinylidene fluoride (PVDF)	MWCN, carboxylic functionalized	500.0	Li2008Fig5b.inp
59	Li (2008) [26]	Polyvinylidene fluoride (PVDF)	MWCN, ester functionalized	500.0	Li2008Fig5c.inp
60	Fan (2012) [27]	Polyvinylidene fluoride (PVDF)	Graphene sheets	100. No data.	Fan2012Fig8.inp
61	Wang (2005) [33]	polyvinylidene / fluoride (PVDF)	multiwall carbon nanotubes (MWNT)	500 No data.	Wang2005Fig1a.inp
62	Dang (2007b) [34]	polyvinylidene fluoride (PVDF)	Functionalized multiwalled carbon-nanotube	500.0	Dang2007bFig3a.inp
63	Sedlakova (2014) [42]	Ethylene-octene copolymer	multiwall carbon nanotubes MWCNT	200.0	Sedlakova2014MWCNT.inp
64	Sedlakova (2014) [42]	Ethylene-octene copolymer	carbon fibers (CF)	66.7	Sedlakova2014CF.inp
65	Jang (2020) [43]	IN2 Epoxy Infusion Resin	carbon nanotube (CNT)	7000.0	Jang2020Fig2a.inp

# Dielectric constant data
	Reference	Matrix material	Filler material	Aspect ratio	File name
66	Sanchez (2018) [5]	Chitosan	Hydroxyapatite nanoparticles	1.0	Sanchez2018Fig7b.inp
67	Wang (2012) [7]	PVDF	Fe3O4	1.0	Wang2012Fig4Permit100Hz.inp
68	Castillo (2022) [19]	Chitosan (CS)	Titanium dioxide nanoparticles	1.0	Castillo2022Fig6.inp
69	Prokhorov (2023) [20]	Chitosan	Graphene oxide sheets, water 24%	150.0	Prokhorov2023Fig5bW24.inp
70	Prokhorov (2023) [20]	Chitosan	Graphene oxide sheets, water 9%	150.0	Prokhorov2023Fig5bW24.inp
71	Prokhorov (2020) [21]	Chitosan	Zinc oxide nanoparticles	1.0	Prokhorov2020Fig4b.inp
72	Chen (2007) [24]	β-polyvinylidene fluoride	Acetylene black	1.0	Chen2007Fig2.inp
73	Dang (2003) [25]	Polyvinylidene fluoride	BaTiO3 particles	1.0	Dang2003Fig2.inp
74	Dang (2003) [25]	Polyvinylidene fluoride and BaTiO3 particles at 0.2 vol. fraction	Multi-walled carbon nanotubes	700.0	Dang2003Fig3.inp
75	Li (2008) [26]	Polyvinylidene fluoride (PVDF)	Multi-walled carbon nanotubes (MWCN)	2000.0	Li2008Fig8a.inp
76	Li (2008) [26]	Polyvinylidene fluoride (PVDF)	MWCN, carboxylic functionalized	500.0	Li2008Fig8b.inp
77	Li (2008) [26]	Polyvinylidene fluoride (PVDF)	MWCN, ester functionalized	500.0	Li2008Fig8c.inp
78	Fan (2012) [27]	Polyvinylidene fluoride (PVDF)	Graphene sheets	100. No data	Fan2012Fig9.inp
79	Yu (2012) [28]	biodegradable poly(butylene succinate)	Natural graphite mineral	1000.0	Yu2012Fig4.inp
80	Min (2013) [29]	Bisphenol type epoxy resin	Graphite nanoplatelets	500.0?	Min2013Fig4a.inp
81	Tang (2011) [30]	Polyvinylidene fluoride (PVDF)	Zirconate titanate nanowires	13.75	Tang2011Fig4NW.inp
82	Tang (2011) [30]	Polyvinylidene fluoride (PVDF)	Zirconate titanate nanorods	3.0	Tang2011Fig4NR.inp
83	Yao (2007) [31]	ferroelectric polyvinylidene fluoride (PVDF)	Multiwall carbon nanotube (MWNT)	62.0	Yao2007Fig2a1.inp
84	Yao (2007) [31]	ferroelectric polyvinylidene fluoride (PVDF)	Multiwall carbon nanotube (MWNT)	116.0	Yao2007Fig2a2.inp
85	Yao (2007) [31]	ferroelectric polyvinylidene fluoride (PVDF)	Multiwall carbon nanotube (MWNT)	437.0	Yao2007Fig2a3.inp
86	Yao (2007) [31]	ferroelectric polyvinylidene fluoride (PVDF)	Multiwall carbon nanotube (MWNT)	833.0	Yao2007Fig2a4.inp
87	Dang (2007a) [32]	ferroelectric polyvinylidene fluoride (PVDF)	Upright carbon fiber (CF)	12.0	Dang2007aFig2.inp
88	Wang (2005) [33]	polyvinylidene fluoride (PVDF)	multiwall carbon nanotubes (MWNT)	500 No data	Wang2005Fig2a.inp
89	Dang (2007b) [34]	polyvinylidene fluoride (PVDF)	Functionalized multiwalled carbon-nanotube	500.0	Dang2007bFig3b.inp
90	Obrzut (2001) [35]	poly(ethylene glycol) diacrylate (PEGDA)	BaTiO3	1.0	Obrzut2001Fig2PEGDA.inp
91	Obrzut (2001) [35]	Trimethylolpropane triacrylate (TMPTA)	BaTiO3	1.0	Obrzut2001Fig2TMPTA.inp
92	Hu (2007) [36]	thermoplastic cyclic olefin copolymer (COC)	barium strontium titanate (BST), micrometer-size	1.0	Hu2007Fig2a.inp
93	Hu (2007) [36]	thermoplastic cyclic olefin copolymer (COC)	barium strontium titanate (BST), nanometer-size	1.0	Hu2007Fig2b.inp
94	Castles (2016) [37]	acrylonitrile butadiene styrene (ABS)	BaTiO3	1.0	Castles2016Fig4a.inp
95	Chen (2005) [38]	epoxy resin	carbonyl-iron-particles (CIPs)	1.0	Chen2005Fig3a.inp
96	Rao (2000) [39]	comercial epoxy resin (Shipley photoepoxy (ε=3))	Lead magnesium niobate-lead titanate (PMN-PT) ceramic particles	1.0	Rao2000comp1.inp
97	Rao (2000) [39]	in-house developed epoxy (ε=4)	Lead magnesium niobate-lead titanate (PMN-PT) ceramic particles	1.0	Rao2000comp2.inp
98	Fu (20022) [40]	High Temp UV resin	A12O3 large particles	1.0	Fu2022Fig7cALL.inp
99	Fu (20022) [40]	High Temp UV resin	A12O3 small particles	1.0	Fu2022Fig7cALS.inp
100	Fu (20022) [40]	High Temp UV resin	BaTiO3 large particles	1.0	Fu2022Fig7cBTL.inp
101	Fu (20022) [40]	High Temp UV resin	BaTiO3 small particles	1.0	Fu2022Fig7cBTS.inp
102	Fu (20022) [40]	High Temp UV resin	SrTiO3 large particles	1.0	Fu2022Fig7cSTL.inp
103	Fu (20022) [40]	High Temp UV resin	SrTiO3 small particles	1.0	Fu2022Fig7cSTS.inp
104	Agrawal (2014) [41]	Thermoset resin epoxy LY 556	micro-sized aluminium nitride (AlN) particles	1.0	Agrawal2014Fig8a.inp
105	Agrawal (2014) [41]	Polypropylene (PP)	micro-sized aluminium nitride (AlN) particles	1.0	Agrawal2014Fig8b.inp

# References
1. Agari, Y., Ueda, A., & Nagai, S. (1991). Thermal conductivity of a polyethylene filled with disoriented short‐cut carbon fibers. Journal of Applied Polymer Science, 43(6), 1117-1124.
2. Aribou, N., Nioua, Y., Bouknaitir, I., El Hasnaoui, M., Achour, M. E., & Costa, L. C. (2019). Prediction of filler/matrix interphase effects on AC and DC electrical properties of carbon reinforced polymer composites. Polymer Composites, 40(1), 346-352.
3. Landauer, R. (1952). The electrical resistance of binary metallic mixtures. Journal of applied physics, 23(7), 779-784.
4. Wu, J., & McLachlan, D. S. (1997). Percolation exponents and thresholds obtained from the nearly ideal continuum percolation system graphite-boron nitride. Physical review B, 56(3), 1236.
5. Sanchez, A. G., Prokhorov, E., Luna-Barcenas, G., Mora-García, A. G., Kovalenko, Y., Rivera-Muñoz, E. M., ... & Buonocore, G. (2018). Chitosan-hydroxyapatite nanocomposites: Effect of interfacial layer on mechanical and dielectric properties. Materials Chemistry and Physics, 217, 151-159.
6. Jang, S. H., & Yin, H. (2015). Effective electrical conductivity of carbon nanotube-polymer composites: a simplified model and its validation. Materials Research Express, 2(4), 045602.
7. Wang, X., Li, W., Luo, L., Fang, Z., Zhang, J., & Zhu, Y. (2012). High dielectric constant and superparamagnetic polymer‐based nanocomposites induced by percolation effect. Journal of applied polymer science, 125(4), 2711-2715.
8. Chiarello, M., & Zinno, R. (2005). Electrical conductivity of self-monitoring CFRC. Cement and Concrete Composites, 27(4), 463-469.
9. Mamunya, Y. P., Davydenko, V. V., Pissis, P., & Lebedev, E. V. (2002). Electrical and thermal conductivity of polymers filled with metal powders. European polymer journal, 38(9), 1887-1897.
10. Kim, Y. J., Shin, T. S., Do Choi, H., Kwon, J. H., Chung, Y. C., & Yoon, H. G. (2005). Electrical conductivity of chemically modified multiwalled carbon nanotube/epoxy composites. Carbon, 43(1), 23-30.
11. Barrau, S., Demont, P., Perez, E., Peigney, A., Laurent, C., & Lacabanne, C. (2003). Effect of palmitic acid on the electrical conductivity of carbon nanotubes− epoxy resin composites. Macromolecules, 36(26), 9678-9680.
12. Clingerman, M. L., King, J. A., Schulz, K. H., & Meyers, J. D. (2002). Evaluation of electrical conductivity models for conductive polymer composites. Journal of Applied Polymer Science, 83(6), 1341-1356.
13. Mamunya, E. P., Davidenko, V. V., & Lebedev, E. V. (1996). Effect of polymer-filler interface interactions on percolation conductivity of thermoplastics filled with carbon black. Composite Interfaces, 4(4), 169-176.
14. Gojny, F. H., Wichmann, M. H., Fiedler, B., Kinloch, I. A., Bauhofer, W., Windle, A. H., & Schulte, K. (2006). Evaluation and identification of electrical and thermal conduction mechanisms in carbon nanotube/epoxy composites. Polymer, 47(6), 2036-2045.
15. Maiti, S., Shrivastava, N. K., & Khatua, B. B. (2013). Reduction of percolation threshold through double percolation in melt‐blended polycarbonate/acrylonitrile butadiene styrene/multiwall carbon nanotubes elastomer nanocomposites. Polymer composites, 34(4), 570-579.
16. Yousefi, N., Gudarzi, M. M., Zheng, Q., Aboutalebi, S. H., Sharif, F., & Kim, J. K. (2012). Self-alignment and high electrical conductivity of ultralarge graphene oxide–polyurethane nanocomposites. Journal of Materials Chemistry, 22(25), 12709-12717.
17. Stankovich, S., Dikin, D. A., Dommett, G. H., Kohlhaas, K. M., Zimney, E. J., Stach, E. A., ... & Ruoff, R. S. (2006). Graphene-based composite materials. Nature, 442(7100), 282-286.
18. Zhang, H. B., Zheng, W. G., Yan, Q., Yang, Y., Wang, J. W., Lu, Z. H., ... & Yu, Z. Z. (2010). Electrically conductive polyethylene terephthalate/graphene nanocomposites prepared by melt compounding. Polymer, 51(5), 1191-1196.
19. Castillo, B. E., Prokhorov, E., Luna-Bárcenas, G., & Kovalenko, Y. (2022). Potential Use of Chitosan-TiO2 Nanocomposites for the Electroanalytical Detection of Imidacloprid. Polymers, 14(9), 1686.
20. Prokhorov, Y., Luna-Barcenas, G., & Kovalenko, Y. (2023). Interphase percolation phenomena in chitosan-graphene oxide nanocomposites, the role of water content. Express Polymer Letters, 17(1).
21. Prokhorov, E., Luna-Bárcenas, G., Yáñez Limón, J. M., Gómez Sánchez, A., & Kovalenko, Y. (2020). Chitosan-ZnO nanocomposites assessed by dielectric, mechanical, and piezoelectric properties. Polymers, 12(9), 1991.
22. Prokhorov, E., España-Sánchez, B. L., Luna-Bárcenas, G., Padilla-Vaca, F., Cruz-Soto, M. E., Vázquez-Lepe, M. O., ... & Elizalde-Peña, E. A. (2019). Chitosan/copper nanocomposites: Correlation between electrical and antibacterial properties. Colloids and Surfaces B: Biointerfaces, 180, 186-192.
23. Sánchez, A. G., Prokhorov, E., Luna-Barcenas, G., Kovalenko, Y., Rivera-Muñoz, E. M., Raucci, M. G., & Buonocore, G. (2019). Effect of Chemical Oxidation Routes on the Properties of Chitosan-MWCNT Nanocomposites. Current Nanoscience, 15(6), 618-625.
24. Chen, Q., Du, P., Jin, L., Weng, W., & Han, G. (2007). Percolative conductor/polymer composite films with significant dielectric properties. Applied Physics Letters, 91(2).
25. Dang, Z. M., Fan, L. Z., Shen, Y., & Nan, C. W. (2003). Dielectric behavior of novel three-phase MWNTs/BaTiO3/PVDF composites. Materials Science and Engineering: B, 103(2), 140-144.
26. Li, Q., Xue, Q., Hao, L., Gao, X., & Zheng, Q. (2008). Large dielectric constant of the chemically functionalized carbon nanotube/polymer composites. Composites Science and Technology, 68(10-11), 2290-2296.
27. Fan, P., Wang, L., Yang, J., Chen, F., & Zhong, M. (2012). Graphene/poly (vinylidene fluoride) composites with high dielectric constant and low percolation threshold. Nanotechnology, 23(36), 365702.
28. Yu, L., Zhang, Y., Tong, W., Shang, J., Shen, B., Lv, F., & Chu, P. K. (2012). Green dielectric materials composed of natural graphite minerals and biodegradable polymer. RSC advances, 2(23), 8793-8796.
29. Min, C., Yu, D., Cao, J., Wang, G., & Feng, L. (2013). A graphite nanoplatelet/epoxy composite with high dielectric constant and high thermal conductivity. Carbon, 55, 116-125.
30. Tang, H., Lin, Y., Andrews, C., & Sodano, H. A. (2011). Nanocomposites with increased energy density through high aspect ratio PZT nanowires. Nanotechnology, 22(1), 015702.
31. Yao, S. H., Dang, Z. M., Jiang, M. J., Xu, H. P., & Bai, J. (2007). Influence of aspect ratio of carbon nanotube on percolation threshold in ferroelectric polymer nanocomposite. Applied Physics Letters, 91(21).
32. Dang, Z. M., Wu, J. P., Xu, H. P., Yao, S. H., Jiang, M. J., & Bai, J. (2007). Dielectric properties of upright carbon fiber filled poly (vinylidene fluoride) composite with low percolation threshold and weak temperature dependence. Applied Physics Letters, 91(7).
33. Wang, L., & Dang, Z. M. (2005). Carbon nanotube composites with high dielectric constant at low percolation threshold. Applied physics letters, 87(4).
34. Dang, Z. M., Wang, L., Yin, Y. I., Zhang, Q., & Lei, Q. Q. (2007). Giant dielectric permittivities in functionalized carbon‐nanotube/electroactive‐polymer nanocomposites. Advanced Materials, 19(6), 852-857.
35. Obrzut, J., Noda, N., & Nozaki, R. (2001, October). Broadband dielectric metrology for polymer composite films. In 2001 Annual Report Conference on Electrical Insulation and Dielectric Phenomena (Cat. No. 01CH37225) (pp. 269-272). IEEE.
36. Hu, T., Juuti, J., Jantunen, H., & Vilkman, T. (2007). Dielectric properties of BST/polymer composite. Journal of the European Ceramic Society, 27(13-15), 3997-4001.
37. Castles, F., Isakov, D., Lui, A., Lei, Q., Dancer, C. E., Wang, Y., ... & Grant, P. S. (2016). Microwave dielectric characterisation of 3D-printed BaTiO3/ABS polymer composites. Scientific reports, 6(1), 22714.
38. Chen, P., Wu, R. X., Zhao, T., Yang, F., & Xiao, J. Q. (2005). Complex permittivity and permeability of metallic magnetic granular composites at microwave frequencies. Journal of Physics D: Applied Physics, 38(14), 2302.
39. Rao, Y., Qu, J., Marinis, T., & Wong, C. P. (2000). A precise numerical prediction of effective dielectric constant for polymer-ceramic composite based on effective-medium theory. IEEE Transactions on Components and Packaging Technologies, 23(4), 680-683.
40. Fu, Y., Li, W., Xu, M., Wang, C., Zhang, L. and Zhang, G., 2022. Dielectric Properties and 3D-Printing Feasibility of UV-Curable Resin/Micron Ceramic Filler Composites. Advances in Polymer Technology, 2022.
41. Agrawal, A., & Satapathy, A. (2014). Effects of aluminium nitride inclusions on thermal and electrical properties of epoxy and polypropylene: an experimental investigation. Composites Part A: Applied Science and Manufacturing, 63, 51-58.
42. Sedláková, Z., Clarizia, G., Bernardo, P., Jansen, J. C., Slobodian, P., Svoboda, P., ... & Izak, P. (2014). Carbon nanotube-and carbon fiber-reinforcement of ethylene-octene copolymer membranes for gas and vapor separation. Membranes, 4(1), 20-39.
43. Jang, S. H., & Li, L. Y. (2020). Self-sensing carbon nanotube composites exposed to glass transition temperature. Materials, 13(2), 259.